## Slide 1
Versatile cell for in-situ RXD investigation of solid/liquid interfaces in photo- and electro-chemical conditions
Dr. Axel Wilson
Dr. Hadeel Hussain
Dr. Jörg Zegenhagen
Prof Chris Nicklin
Mr. Immad Nadeem
Prof. Geoff Thornton
Diamond Light Source
University College London
Notes: I’m going to present the development of a new device available on the I07 beamline at DLS (which is the British national 3rd generation synchrotron) and in partnership with UCL
This device purpose is to allow the combination of SXRD at the interface solid/liquid in photo and/or electrochemical conditions.
After a short introduction I will present the main features of the cell and the technological solution we adopted
I will the name a couple of example where this cell would be a decisive addition
I will finally present the first experiment we did with the cell

## Slide 2
Introduction: physico-chemistry of interfaces in ‘real’ conditions
Physico-chemistry of surfaces ⇒ evidence and explain phenomena occurring at surfaces and interfaces
2
Model conditions
Real conditions
VS
Simplify the interpretation
Theoretically easier to investigate
Make the system compatible with specific investigation method
Closer to development phase
May involve new, complex mechanisms
Notes: One of the objective of surface science is to evidence and explain reactions/phenomena occurring at interfaces
We can however distinguish studies realized on model conditions (in vacuum, at room temperature, at 0K in the case of theoretical studies) or real conditions (atmospheric or high pressure, high temperature)
Working on a model system allow to isolate as much as possible the system and study precisely one given phenomenon and facilitate the interpretation.
In terms of computational science it is sometime necessary to use model conditions to decrease computing time.
Some investigation technique require these condition to operate. XPS and LEED for example have to be realized in vacuum to collect electrons with the analyser, STM is much more stable in vacuum than in atmospheric pressure of reactant.
On the other hand real condition allow to work much closer to what would be the conditions in the development phase of a system.
It may, however, involve additional phenomena/reactions that complexity drastically the interpretation for a give observation

## Slide 3
Introduction: physico-chemistry of interfaces in ‘real’ conditions
Physico-chemistry of surfaces ⇒ evidence and explain phenomena occurring at surfaces and interfaces
2
Real conditions
VS
Pressure gap
Material gap
Closer to development phase
May involve new, complex mechanisms
→ Near ambient pressure XPS
→ Ambient pressure / liquid phase STM
→ Environmental HRTEM
Model conditions
Simplify the interpretation
Theoretically easier to investigate
Make the system compatible with specific investigation method
Notes: In surface science we even have a word to describe the fact of transiting from model conditions to real conditions. Bridging the pressure/material gap.
To overcome this difficulty talented researcher have adapted some of the techniques used on model system with among others NAPXPS, AP LP STM (ambient pressure means here performing STM in a controlled environment) or E-HRTEM where a small cell with gas inlet and outlet is used to separate vacuum from reactive environment.

## Slide 4
Introduction: physico-chemistry of interfaces in ‘real’ conditions
Physico-chemistry of surfaces ⇒ evidence and explain phenomena occurring at surfaces and interfaces
2
Real conditions
VS
Pressure gap
Material gap
Closer to development phase
May involve new, complex mechanisms
→ Near ambient pressure XPS
→ Ambient pressure / liquid phase STM
→ Environmental HRTEM
Reactions at the solid/liquid interface are difficult to study due to the high absorption of the liquid phase
→ Structural investigation using Surface X-ray Diffraction (ν > 10 keV)
→ Development of a versatile cell for multi environmental purpose
Model conditions
Simplify the interpretation
Theoretically easier to investigate
Make the system compatible with specific investigation method
Notes: Solid/liquid interfaces are not compatible with most of the standard investigation technique mentioned previously due to the high absorption of the layer of liquid.
XRD using hard X-ray generated with

## Slide 5
Main features:
UHV preparation, pre-characterisation and transfer to I07 diffractometer
→ Preparation using standard UHV procedures
→ Pre-characterisation using VT-STM, monochromated XPS and LEED
→ Allows to perform offline experiments
XRD PECcell body
30 cm
XRD photo-electrochemical cell
3
Notes: I will now present the XRD photo-electrochemical cell insisting on the features available on the latest version.
The first important feature is that the cell is UHV compatible and can be mounted directly on a UHV apparatus.

## Slide 6
Main features:
UHV preparation, pre-characterisation and transfer to I07 diffractometer
XRD photo-electrochemical cell
→ Preparation using standard UHV procedures
→ Pre-characterisation using VT-STM, monochromated XPS and LEED
→ Allows to perform offline experiments
PECcell body
Beryllium
cylinder
3

## Slide 7
Main features:
UHV preparation, pre-characterisation and transfer to I07 diffractometer
Formation of a solid/liquid interface
Introduction of the liquid delivery device
Liquid is handled using a dual syringe pump
→ Dispense fresh electrolyte
→ Pick-up from the interface
→ Possibility to flow the electrolyte
Interface monitored using an endoscope and camera
Electrolyte out
Electrolyte in
Sample
XRD photo-electrochemical cell
Design based on F. U. Renner, Y. Gruender & J. Zegenhagen, Rev. Sci. Inst., 78, 2007
4

## Slide 8
Main features:
UHV preparation, pre-characterisation and transfer to I07 diffractometer
Formation of a solid/liquid interface
Application of an external potential
The sample (working electrode) is isolated from ground
A platinum electrode is located inside the inner capillary
A reference electrode is located over the capillaries
Cyclic voltammetry and chronoamperometry with Ivium potentiostat
Platinum electrode
Reference
electrode
Camera
Working electrode
XRD photo-electrochemical cell
5
Design based on F. U. Renner, Y. Gruender & J. Zegenhagen, Rev. Sci. Inst., 78, 2007

## Slide 9
Main features:
UHV preparation, pre-characterisation and transfer to I07 diffractometer
Formation of a solid/liquid interface
Application of an external potential
The sample (working electrode) is isolated from ground
A platinum electrode is located inside the inner capillary
A reference electrode is located over the capillaries
Cyclic voltammetry and chronoamperometry with Ivium potentiostat
XRD photo-electrochemical cell
5

## Slide 10
Main features:
UHV preparation, pre-characterisation and transfer to I07 diffractometer
Formation of a solid/liquid interface
Application of an external potential
Illumination of the sample
The sample can be illuminated trough the glass-to-metal reducer
Intense LED-UV light (365nm 10mA.cm-2) is available at the moment
UV LED
Cooling block
XRD photo-electrochemical cell
6

## Slide 11
Main features:
UHV preparation, pre-characterisation and transfer to I07 diffractometer
Formation of a solid/liquid interface
Application of an external potential
Illumination of the sample
Operate entirely from the control cabin of the beamline
A unique computer controlling the cell can be remote accessed
→ Syringe pump
→ Potentiostat
→ UV illumination system
→ Monitoring camera
Interface monitor
Syringe control
Potentiostat software
Syringe status
XRD photo-electrochemical cell
7

## Slide 12
Surface X-ray Diffraction: basics
Experience realized at grazing incidence close to the critical angle to improve surface sensitivity
Surface X-Ray Diffraction (SXRD)
Structure of crystalline surfaces
Displacements, roughness, surface relaxation
Grazing Incidence X-ray Diffraction (GIXD)
Structure of nano-objects
Size, lattice parameters, strains, domains
Grazing Incidence Small Angle X-ray Scattering (GISAXS)
Morphology of nanostructures
Size, size distribution, shape
Particle-particle pair correlation function
HDR, Giles Renaud, CEA, 2011
w
D
h
d
ai
ki
af
2q
qx
qz
qy
GISAXS
2D detector
2D detector
2q
SXRD
& GIXD
slits
Q//
Q
af
d
kf
8

## Slide 13
Surface X-ray Diffraction: example of application
9
In-situ growth of bimetallic NPs using deposition precipitation
Nano Today 7, 2012

## Slide 14
Surface X-ray Diffraction: example of application
9
In-situ growth of bimetallic NPs using deposition precipitation
Structural evolution of the interface during solid/liquid (photo-)catalysis: activation and deactivation
Nano Today 7, 2012
Industrial & Engineering Chemistry Research 48, 2009

## Slide 15
Surface X-ray Diffraction: example of application
9
In-situ growth of bimetallic NPs using deposition precipitation
Structural evolution of the interface during solid/liquid (photo-)catalysis: activation and deactivation
Operando evolution of a metal-oxide electrode during photo-electrocatalytic water splitting
Chemical Society review 43, 2014
Nano Today 7, 2012
Industrial & Engineering Chemistry Research 48, 2009

## Slide 16
Solid/liquid interfaces TiO2/NaOH(0.1M) and TiO2/HCl(0.1M)
Sample prepared in UHV, characterized using STM, LEED and XPS
Transferred in UHV to the diffractometer, characterized using SXRD
Vented to N2 before formation of the interfaces
NaT
NaB
Ti5c
OA
OT
O2c
Rutile TiO2(110)/NaOH(0.1M)
Rutile TiO2(110)/HCl(0.1M)
→ A monolayer of Terminal O (Ot) species exist.
→ A monolayer of NaT which interacts with four O, adsorbs in a tetra-dentate Site.
→ A monolayer of NaB which interacts with four O, adsorbs in a tetra-dentate Site.
→ A monolayer of O species above the Na exists.
10

## Slide 17
Solid/liquid interfaces TiO2/NaOH(0.1M) and TiO2/HCl(0.1M)
Sample prepared in UHV, characterized using STM, LEED and XPS
Transferred in UHV to the diffractometer, characterized using SXRD
Vented to N2 before formation of the interfaces
NaT
NaB
Ti5c
OA
OT
O2c
Rutile TiO2(110)/NaOH(0.1M)
Rutile TiO2(110)/HCl(0.1M)
ClT
→ A monolayer of Terminal Cl (Clt) species exist.
→ A monolayer of O species above the Cl exists.
→ A monolayer of Terminal O (Ot) species exist.
→ A monolayer of NaT which interacts with four O, adsorbs in a tetra-dentate Site.
→ A monolayer of NaB which interacts with four O, adsorbs in a tetra-dentate Site.
→ A monolayer of O species above the Na exists.
OA
Ti5c
O2c
10

## Slide 18
For any question regarding the XRD photo-electrochemical cell
Dr. Axel Wilson (axel.wilson@diamond.ac.uk)
For any question about I07 beamline and beamtime application
Prof. Chris Nicklin (I07 principal beamline scientist, chris.nicklin@diamond.ac.uk)
Looking forward to seeing you at Diamond Light Source, Oxfordshire, UK!
Acknowledgement:
Immad Nadeem (Phd student)
Dr. Hadeel Hussain (Post-doc)
Prof. Geoff Thornton (UCL)
Adam Warne (Technician)